## Slide 1: Hydrogenation Of SRBDPS for P-12
Feed material : SRBDPS | 
Product: P-12 | 
Batch Size: 7.5 MT | 
Initial IV: 34 | 
Required IV : 0.7 | 
Catalyst quantity : 20 KG | 

## Slide 2: Case no.01 : As per regular procedure
Previously we were dropping the batch after 3 hrs. but from this experiment it has been concluded that we can drop batch after 2.33 hrs. (after hydrogen starts).
Product | Batch charging | Catalyst addition | Hydrogenation + Hold up | Batch transfer | Valve operation | Venting | Total Time in Min | Total Time in Hr | Batch/Day
P-12 | 10 | 15 | 180 | 30 | 22 | 15 | 270 | 4.5 | 10.66
 |  |  | After |  |  |  |  |  | 
P-12 | 10 | 15 | 140 | 30 | 22 | 15 | 232 | 3.9 | 12.30

## Slide 3: Case No. 2 By Flip
Starting Hydrogen gas to the reactor & after 15-17 mints we vent/flip Hydrogen/ Inerts for 3 mints but satisfactory results were not found ( as compared to normal procedures).
Batch No | 21185 | 21186 | 21187 | 21188
 | IV | IV | IV | IV
Time min |  |  |  | 
20 | 1.31 | 2.34 | 1.08 | 1.21
40 | 0.89 | 0.81 | 0.79 | 0.87
60 | 0.91 | 0.71 | 0.9 | 0.83
80 | 0.76 | 0.7 | 0.84 | 0.79
100 | 0.71 | 0.64 | 0.85 | 0.81
120 | 0.66 | 0.64 | 0.82 | 0.72
140 |  |  | 0.64 | 0.75

## Slide 4: Case No.3 Addition of catalyst at various Temperatures.
It has been observed that up to 170 0 C temperatures results are getting satisfactory. Above 170 o C catalyst may deteriorated.
Batch No | 21177 | 21178 | 21179 | 21180 | 21181 | 21182 | 21183 | 21184
Temp. Deg. C | 148.88 | 155.33 | 158.83 | 162.9 | 170.97 | 170.43 | 178.15 | 179.27
Time in mints | IV | IV | IV | IV | IV | IV | IV | IV
20 | 0.96 | 1.03 | 1.12 | 0.85 | 0.77 | 4.0 | 1 | 1.04
40 | 0.71 | 0.69 | 0.76 | 0.71 | 0.7 | 1.04 | 0.78 | 0.8
60 | 0.64 | 0.62 | 0.69 | 0.62 | 0.59 | 0.7 | 0.76 | 0.78
80 | 0.62 | 0.69 | 0.69 | 0.68 | 0.59 | 0.65 | 0.75 | 0.76
100 | 0.59 | 0.64 | 0.71 | 0.61 | 0.58 | 0.64 | 0.74 | 0.85
120 |  |  |  | 0.66 | 0.57 | 0.61 | 0.74 | 0.76

## Slide 5: Discharge time should be 6 min. instead of 35 min.
Location of control valve is wrong, need to be relocate ( nearest to V-702) then vibration issue will solve and we can transfer batch faster.

## Slide 6: 9 mt batch during UTSR run
It is not possible to take 9 mt batch, because it Exide the actual volume of reactor.